Investigation of physico-chemical properties of gelatin matrices in correlation with dissolution studies

MN Hattrem, KI Draget

Norwegian Biopolymer Laboratory (NOBIPOL), Department of Biotechnology, Norwegian University of science and Technology, N-7491 Trondheim, Norway

Gelatin is commonly used in formulation of pharmaceuticals and nutraceuticals, either as soft or hard gel capsules. Most recently a new type of gelatin based formulation has been proposed1. For all these applications the dissolution profile of the matrix in the gastrointestinal tract is of crucial importance. Dissolution studies are generally time consuming and it would hence be advantageous to be able to predict the dissolution profile by evaluating the physico-chemical properties of the gelatin matrix. In this study, gelatin matrices were prepared with varying bloom and chemical composition (type A and B). Dissolution profiles were recorded applying a standard pharmaceutical dissolution unit/procedure (Sotax AT 7smart, 0.1 M HCl, 37 °C, 50 RPM, Basket) using acetaminophen as a marker. The physio-chemical properties of the gelatins were determined by the use of Size-exclusion chromatography multiangle light scattering (SEC-Malls) for determination of molecular weight distribution. Determination of isoelectric point (pI) by acid-base titration combined with zeta-potential measurement and rheological characterization by small strain oscillatory measurements.

Preliminary results suggest a correlation between the rheological properties, molecular weight distribution and the corresponding dissolution profile of the gel.

References:

1 Haug, I. J., Sagmo, L. B., Zeiss, D., Olsen, I. C., Draget, K. I. & Seternes, T. 2011. Bioavailability of EPA and DHA delivered by gelled emulsions and soft gel capsules. European Journal of Lipid Science and Technology, 113, 137-145.

Poster presentation is prefered