Biochemical, chemical and rheological properties of Detarium microcarpum and Irvingia gabonensis seed flours

Kate E. Nwokocha1,*, Louis. M. Nwokocha2, Peter A. Williams3

1Department of Biohemistry, University of Ibadan, Ibadan, Nigeria

2Department of Chemistry, University of Ibadan, Ibadan, Nigeria

3Center for Water Soluble Polymers, Glyndwr University, Wrexham,

North Wales LL 11 2AW, UK

*Abstract. presenting- kenwokocha@yahoo.com

Seed flours of two tropical food thickeners: Detarium microcarpum and Irvingia gabonensis were studied. The proximate composition, metal contents and antioxidant properties were determined.

The rheological properties of 5% flour pastes showed that Detarium microcarpum flour paste with zero shear viscosity (ηo = 56.69 Pa s) had superior thickening power than Irvingia gabonensis (ηo = 14.8 Pa s).  Detarium microcarpum flour paste exhibited properties of entangled network with G’ = G” at ω = 20.92 rad/s and G” > G’ at lower frequencies while Irvingia  gabonensis was elastic with G’ > G” at all frequencies.

Key words: Detarium microcarpum, Irvingia gabonensis, flour, metal content, antioxidant properties, rheological properties

Viscosity-shear rate profiles of 5% aqueous dispersions of Detarium microcarpum and Irvingia gabonensis  flour pastes at 25oC

Frequency sweep showing G’ and G” of 5% aqueous dispersions of Detarium microcarpum and Irvingia gabonensis  flour pastes at 25oC