Protein stabilised foams; stability and rheological properties

A Lazidis1, RD Hancocks1, R Berrocal2, IT Norton1

1Department of Chemical Engineering, University of Birmingham, Edgbaston B15 2TT, United Kingdom

2Nestlé Product Technology Centre, 3510 Konolfingen, Switzerland

Many food products are composed of a gas dispersed phase widely known as foam. Some examples are cappuccinos, mousses and milk shakes. Foams are thermodynamically unstable systems, as they are prone to drainage, coalescence and disproportionation (similar to Ostwald ripening for emulsions) and generally have a lifetime of some orders of magnitude smaller than that of emulsions (hours compared to months) 1. A common way of stabilising foams is by the use of proteins. The mechanism of foam formation and stability has been the focus of attention since the beginning of industrial processing of milk.

In this study, the mechanism of foam stabilisation by proteins and their structures is being described focusing on the effect that different protein types and external conditions have on the mechanical properties of the interfacial films. Model systems containing different milk protein sources, whey protein isolate (WPI) and micellar milk protein isolate (MPI), at different concentrations were studied. The effect of conditions like pH, temperature and ionic strength on foaming and foam stability was also investigated. The stability of protein foams under different conditions was hence studied using the traditional method2 where foam is being produced and the density and volume is recorded over time. Additionally, a more automated method3 was employed where the electrical conductivity of the created foam is recorded at different heights of its volume over time giving important information on the liquid fraction of the foam and the kinetics of instability. The effect of the type and concentration of protein and the environmental conditions on the bulk rheological properties is demonstrated in terms of elastic (G’) and viscous (G’’) modulus and apparent viscosity (ηα). Furthermore, the rheological properties of the foams4 were also measured in terms of G’ and G’’ by using dynamic oscillatory techniques and also the yield stress (τγ) and ηα obtained from stress ramps. An investigation on the rheological properties of the air/water interface by the use of interfacial shear rheology with a Du Noüy ring is also shown and discussed. Finally, an overview of the associations between the bulk and interfacial mechanical properties of the suspensions and their foams and the stability of the foams is illustrated and explained.

References:

- Walstra, Pieter. 2003. “Physical Chemistry of Foods”. CRC Press.

- Waniska, R. D, and J. E Kinsella. “Foaming Properties of Proteins: Evaluation of a Column Aeration Apparatus Using Ovalbumin.” Journal of Food Science 44, no. 5 (September 1, 1979): 1398–1402.

- Kato, Akio, Atsunobu Takahashi, Naotoshi Matsudomi, and Kunihiko Kobayashi. “Determination of Foaming Properties of Proteins by Conductivity Measurements.” Journal of Food Science 48, no. 1 (January 1, 1983): 62–65.

- Jimenez-Junca, Carlos A., Jean C. Gumy, Alexander Sher, and Keshavan Niranjan. “Rheology of Milk Foams Produced by Steam Injection.” Journal of Food Science 76, no. 9 (November 2011): E569–E575.