Solution properties of Brachystegia eurycoma seed polysaccharide

Louis M. Nwokocha1,* , Peter A. Williams2

1Department of Chemistry, University of Ibadan, Ibadan, Nigeria

2Center for Water Soluble Polymers, Glyndwr University, Wrexham,

North Wales LL 11 2AW, UK

*Abstract. presenting- lm.nwokocha@mail.ui.edu.ng

Abstract

Brachystegia eurycoma seed endosperm is an important food thickener in the sub-Saharan Africa. We have isolated the polysaccharide component of the seed endosperm at a yield of 44.3% and studied its solution properties. The polysaccharide had a weight average molecular weight (Mw) of 5.4 x 105 g/mol and intrinsic viscosity of 4.3 dl/g. The viscosity-shear rate profiles showed that the rheological properties of the polysaccharide were dominated by viscous flow in the dilute to moderately concentrated solutions. A complete treatment of the viscosity over the entire concentration range was obtained by a log-log plot of the zero shear specific viscosity, ηsp, versus volume concentration, c[η] and the result fitted to different viscosity models. The flow properties of the polysaccharide were temperature dependent. The activation energy (Ea) for viscous flow determined from Arrhenius plot of zero shear viscosity versus inverse of absolute temperature (Figure 1) was concentration dependent, with the Ea for 5% polysaccharide (Ea = 30.7 KJ/mol) more than double that for 4% (Ea = 14.04 KJ/mol). Cox-Merz plots gave good superimposition of complex and shear viscosities (Figure 2).

Key words: Brachystegia eurycoma polysaccharide, flow and viscoelastic properties, molecular weight

Acknowledgement: The authors acknowledge the funding support of Leverhulme Trust Foundation.

Figure 1. Arrhenius plots of zero shear viscosity versus inverse of absolute temperature for 4% and 5% concentrations of Brachystegia eurycoma polysaccharide

Figure 2. Cox-Merz plots: Superimposition of dynamic viscosity (η*) versus angular frequency (ω) (opened) and steady shear viscosity (η) versus shear rate (γ) (closed) for Brachystegia eurycoma polysaccharide solutions at 25 oC