Calcium binding and calcium-induced gelation of sodium alginate modified by the addition of low-molecular weight alginate- and pectin-derivatives

M Nakauma1, T Funami1, Y Fang2, K Nishinari2, KI Draget3, and GO Phillips4

1Texture Design Division, San-Ei Gen F.F.I., Inc., 1-1-11, Sanwa-cho, Toyonaka, Osaka 561-8588, Japan

2Glyn O. Phillips Hydrocolloid Research Centre at HUT, School of Food and Pharmaceutical Engineering, Faculty of Light Industry, Hubei University of Technology, Wuchang, Wuhan 430068, China

3Norwegian Biopolymer Laboratory, Department of Biotechnology, Norwegian University of Science and Technology, N-7491 Trondheim, Norway

4Phillips Hydrocolloids Research Ltd., 45 Old Bond Street, London W1S 4AQ, UK

Effects of low-molecular weight alginate- and pectin-derivatives (low-molecular weight polyuronate derivatives) were investigated on the calcium binding and calcium-induced gelation of sodium alginate (ALG) with higher molecurer weight. Low-molecular weight alginate derivatives of two different guluronate contents (Gc) were prepared using acid hydrolysis and subsequent fractionation by changing pH. Low-molecular weight pectin derivatives of two different degrees of methylation (DM) were prepared by two-step enzymatic treatment for hydrolysis and subsequent de-esterification.

For the mixture of ALG and each low-molecular weight polyuronate sample, change in the relative viscosity of dilute solutions upon addition of calcium was measured using an Ubbelohde type capillary viscometer at 25 °C. Either alginate derivative with low Gc (mannuronate rich type; LMw-MAL) or pectin derivative with high DM (LMw-HMP) did not alter significantly the calcium binding behaviour of ALG. On the other hand, alginate derivative with high Gc (guluronate rich type; LMw-GUL) and pectin derivative with low DM (LMw-LMP) altered it greatly although the effects were opposite each other. A larger amount of calcium was required for rapid increase in the relative viscosity, which can be associated with the initiation of the egg-box dimer formation, in the case of LMw-GUL, whereas a smaller amount of calcium was required in the case of LMw-LMP.

Rheological properties of gelled system were investigated using a strain-controlled rheometer with parallel plate geometry at 20 °C. Gels from the mixture of ALG and each LMw polyuronate sample in the presence of calcium carbonate and glucono--lactone were tested. Effects on the rheological properties of ALG gels were also different between LMw-GUL and LMw-LMP. LMw-GUL decreased dynamic storage modulus G' with increased yield strain with increasing addition level, whereas LMw-LMP decreased G' without changing the yield strain with increasing addition level.  These rheological changes can be explained by competitive formation of the egg-box dimers between ALG and low-molecular weight polyuronate sample and also by the structural difference between low-molecular weight polyuronates.

Results obtained should contribute to the best use of low-molecular weight polyuronate sample as a novel texture modifier in alginate system.