CHARACTERIZATION OF A NEW POLYSACCHARIDE FROM COLA MILLENII SEEDS

Louis M. Nwokocha1 and Peter A. Williams2

1Department of Chemistry, University of Ibadan, Ibadan, Nigeria

2Center for Water Soluble Polymers, Glyndwr University, Wrexham,

North Wales LL 11 2AW, UK

Presenting: Email: lm.nwokocha@mail.ui.edu.ng

We have isolated and characterized a new water soluble polysaccharide from Cola millenii seeds. The monosaccharide composition showed it is composed of 59% neutral sugars and 41% uronic acids. It exhibited polyelectrolyte properties with the intrinsic viscosity varying with salt concentration. It has a weight average molecular weight of 4.66 x 106 g/mol. The polysaccharide formed a high viscous solution in water with a zero shear viscosity of 17.91 Pa s at 1% (w/v) polysaccharide solution. The polysaccharide exhibited shear thinning properties even at very low concentrations, The mechanical spectra showed the polysaccharide exhibited elastic properties at 2% concentration suggesting a potential for application as suspending agent and emulsifier.