Synthesis and Characterization of Bacterial Cellulose–Alginate Composites: Influence of Mannuronic and Guluronic Acid Ratios on Hydrogel Structure.

P Cazón1,2, M. Martínez-Sanz3, M. Vallet-Vila1, and P. Lopez-Sanchez4*

1Department of Analytical Chemistry, Faculty of Veterinary, Campus Terra, University of Santiago de Compostela, 27002 Lugo, Spain

2Dairy Products and Food Technology Centre APLTA, Universidade de Santiago de Compostela, Campus Terra, Rúa Montirón, Lugo 27002, Spain

3Instituto de Investigación en Ciencias de la Alimentación, CIAL (CSIC-UAM, CEI UAM + CSIC), Nicolás Cabrera, 9, Madrid, 28049, Spain

4Instituto de Investigaciones Marinas, Consejo Superior de Investigaciones Científicas (CSIC), 36208 Vigo, Spain

Bacterial cellulose (BC), synthesized by Acetobacter species, is a versatile polysaccharide with exceptional mechanical strength, thermal stability, high crystallinity, and barrier properties against water vapor, oxygen, and ultraviolet radiation. These features make BC a promising candidate for applications in food, pharmaceutical, and biomedical sectors1. To enhance its functionality, this study employed in-situ modification by incorporating alginate, a polysaccharide derived from brown seaweed, into the BC culture medium (HS). Alginate, comprising β-D-mannuronic acid (M) and α-L-guluronic acid (G), exhibits physicochemical properties influenced by its M/G ratio and block distribution, which impact behaviors such as gelation and mechanical performance2.

BC–alginate hydrogels were synthesized by integrating alginates with varying M/G ratios during BC biosynthesis. Advanced characterization techniques were used to analyze these composites. Fourier-transform infrared spectroscopy with attenuated total reflectance (ATR-FTIR) identified molecular interactions, small-angle X-ray scattering (SAXS) provided nanoscale structural information, and scanning electron microscopy (SEM) facilitated surface morphology examination. Mechanical and rheological properties were assessed through uniaxial compression tests and small-amplitude oscillatory rheology.

The results demonstrated that the interaction between BC and alginate led to modifications in the structure and properties of the composite, with these changes being dependent on the M/G ratio. Variations in the M/G ratio appeared to influence the mechanical and rheological characteristics of the hydrogels, suggesting a role of the M/G distribution in determining the final material properties.

This research highlights the potential of BC–alginate hydrogels as customizable biomaterials, offering valuable insights into their structural interactions and functional properties.

References:

1	Cazón, P., & Vázquez, M. (2021). Improving bacterial cellulose films by ex-situ and in-situ modifications: a review. Food Hydrocolloids, 113, 106514. https://doi.org/https://doi.org/10.1016/j.foodhyd.2020.106514.

2	Augst, A.D., Kong, H.J. and Mooney, D.J. (2006), Alginate Hydrogels as Biomaterials. Macromol. Biosci., 6: 623-633. https://doi.org/10.1002/mabi.200600069.