Development of chitosan films containing α-, β-, or γ-cyclodextrin inclusion complexes for controlled release of food aroma.

I Zarandona1, C Barba2, P Guerrero1, K de la Caba1 and J Maté2

1 BIOMAT research group, University of the Basque Country (UPV/EHU), Escuela de Ingeniería de Gipuzkoa, Plaza de Europa 1, Donostia-San Sebastian 20018, Spain

2 Department of Agronomy, Biotechnology and Food Science , Public University of Navarre (UPNa), Campus de Arrosadía s/n, Edificio Los Olivos, Pamplona 31006, Spain

There is an increasing use of cyclodextrin (CD) as additive in edible films and coatings. Edible films are well recognized for their potential to be an useful tool to protect food and to increase their quality properties1. The CD can be added as additive in edible films and coatings for many purposes including controlled release, increase molecular stability, protect reactions, reduced off-flavors and add flavors which is especially interesting depending on the specifically food application2. Furthermore, the use of CD may have a synergetic effect in the formation of the edible films that may benefit good technological properties3.

In this work we propose β-cyclodextrin (β-CD) inclusion complexes of a food industry aroma (2-phenylethanol)4 as a controlled release tool for edible films based on chitosan. The work included: i) preparation of α-, β-, and γ-CD:2-phenylethanol inclusion complexes (1:1) by co-precipitation and drying by spray-drying, ii) evaluation of the retention efficiency, iii) preparation and characterization of complexes and films, and; iv) evaluation of the controlled release with and without the use of cyclodextrins in a food simulant.

The FT–IR transmittance spectra obtained with the prepared inclusion complex showed a slight shift of the characteristic band to 3394 cm-1, suggesting the host-guest interaction of the –OH group of the 2-phenylethanol with the C–O–C group of the CD. The retention efficiency of 2-phenylethanol in α-, β-, and γ-CD was 32%, 45% and 40% (molar basis), respectively. Chitosan films containing β-CD:2-phenylethanol inclusion complex were developed and the characterization of the films and complexes was carried out to explain the controlled release.

1 Pavlath, A.E. and Orts, W. (2009). Edible Films and Coatings: Why, What, and How?. Edible films and coatings for food applications, 1-23.

2 Barba, C., Eguinoa, A. and Maté, J. (2015). Preparation and characterization of β-cyclodextrin inclusion complexes as a tool of a controlled antimicrobial release in whey protein edible films. LWT Food Science and Technology, 64, 1362-1369.

3 Youxin, Y. , Mingjin, Z., Keyan, M., Xinying, L., Defu, L. and Changdao, M. (2017). Development of antimicrobial gelatin-based edible films by incorporation of trans-anethole/β-cyclodextrin inclusion complex. Food Bioprocess Technology, 10, 1844 –1853.

4 Zujin, Y., Xingdong, Y., Zuobing,  X., Hongyan, C. and Hongbing, J. (2015). Preparation and release behaviour of the inclusion complexes of phenylethanol with β-cyclodextrin. Flavour and Fragance Journal, 31, 206-216.