Oral Presentation:

A structural and conformational study on non-pectic polysaccharides from water soluble yellow mustard mucilage

Y. Wu1, 3, W. Cui 1, N.A.M. Eskin2 and H.D. Goff3

1Agriculture and Agri-Food Canada, Guelph Food Research Centre, 93 Stone Road West, Guelph, Ontario, N1G 5C9, Canada

2Department of Human Nutritional Science, Faculty of Human Ecology, University of Manitoba, Winnipeg, MB R3T 2N2, Canada

3Department of Food Science, University of Guelph, 50 Stone Road East, Guelph, Ontario, N1G 2W1, Canada

A non-pectic polysaccharide fraction (NPP) isolated from water soluble yellow mustard mucilage (WSM) exhibited unique rheological properties, such as form thermal stable gels and exhibited strong synergism with four galactomannas1. The current paper reports on the further elucidation of its fine structure and conformational properties using methylation analysis, 2D NMR spectroscopy and light scattering techniques. Methyaltion analysis revealed that NPP was mainly composed of 1,4 linked glucose. NMR analysis further confirmed the backbone of this polysaccharide as 1,4 linked beta-D-glucose, and provided evidence confirming the presence of branches along the polysaccharide chain.  Conformational studies by static and dynamic light scattering showed that NPP behaved relatively stiff in aqueous solutions. The information on structure and conformation of this polysaccharide in aqueous solutions will help to understand its unique rheological properties and mechanisms for its interactions with galactomannans.

References

1. Wu, Y., Cui, W. S., Eskin, N.A.M. and Goff, D. (2008) Rheological Investigation of Synergistic Interactions between Galactomannans and  Non-Pectic Polysaccharide Fraction from Water Soluble Yellow Mustard Mucilage. Food hydrocolloids, 2008 (In Press).

2. Cui, W., Eskin, N.A.M. and Biliaderis, C.G. (1995) NMR characterization of a water-soluble 1,4-linked β--glucan having ether groups from yellow mustard (Sinapis alba L.) mucilage. Carbohydrate Polymers 27, 117-122.