Atomic force microscopy studies of the nanomechanical properties of natural oil bodies

Nan Yanga,b,d,*, Chunxia Sua,, Junji Jiac, Robert L. Lehenyd, Katsuyoshi Nishinaria,b, Yapeng Fang a,b

aGlyn O. Phillips Hydrocolloid Research Centre, Department of Bioengineering and Food Science, Hubei University of Technology, Wuhan 430068, China;

bFood Hydrocolloid International Science and Technology Cooperation Base of Hubei Province, Hubei University of Technology, Wuhan 430068, China;

cSchool of Physics and Technology, Wuhan University, Wuhan 430072, China

dDepartment of Physics and Astronomy, Johns Hopkins University, Baltimore, MD 21218, USA

* To whom correspondence should be addressed: Tel, +86 (0) 27-88015996; Fax, +86 (0)27-88015996; Email, nyang19@jhu.edu

Abstract: Oil bodies (OBs) are micrometer-scale oil droplets found in many plant organs. As natural emulsions with remarkable stability, OBs are viewed as promising materials for applications in colloid science, such as energy reservoirs, protein recombination, active agents delivery vehicles, and functional ingredients in foods, cosmetics, and pharmaceuticals [1]. Their interfacial layer, composed of phospholipids with embedded proteins, plays an important role in their physicochemical stability and functions. In this study, the interfacial mechanical properties of OBs from three plant sources--soybean, sesame and peanut -- were investigated in-situ by colloidal probe atomic force microscopy (AFM) [2,3]. Different regions of the force-deformation curves during compression were analyzed using a suite of models, including Hooke’s law, Reissner theory, and the elastic membrane theory [4,5]. We found that the natural OBs are very soft droplets but do not rupture and fully recover following compressive strains ε as large at 0.2 . Over a range of small strains (ε=0.003-0.05), the strain varies linearly with the compressive force, Reissner theory applied in this region yields a Young’s modulus (E) of the OB membranes that is is similar in magnitude to that obtained from the elastic membrane theory at higher strains (ε=0.05-0.10). However, at the highest strains probed in the measurements (ε=0.10-0.20) agreement with elastic membrane theory breaks down. We propose an extension of the theory that includes a contribution to the force from interfacial tension based on the Gibbs energy, allowing effective determination of E and the surface tension of the membrane of the OB droplets in a water environment. Overall, stiffness and E of the soybean OBs were larger than those of sesame and peanut OBs, and both were negatively correlated with OB particle size, which was dictated by the composition and structure of the OB surface membranes.

References:

[1] Nikiforidis, C.V., Matsakidou, A., Kiosseoglou, V. (2014). Composition, properties and potential food applications of natural emulsions and cream materials based on oil bodies. RSC Adv. 4(48): 25067-25078.

[2] Butt, H-J, Cappella, B., Kappl, M. (2005). Force measurements with the atomic force microscope: Technique, interpretation and applications. Surface Science Reports, 59(1-6): 1-152.

[3] Tabor, R. F., Grieser, F., Dagastine, R. R., et al. (2012). Measurement and analysis of forces in bubble and droplet systems using AFM. Journal of Colloid and Interface Science, 371(1): 1-14.

[4] Santos, E. B., Morris, J. K., Glynos, E., et al. (2012). Nanomechanical Properties of Phospholipid Microbubbles[J]. Langmuir, 28(13): 5753-5760.

[5] Lulevich. V., Yang, H-Y, Rivkah, Isseroff, R., et al. (2010). Single cell mechanics of keratinocyte cells. Ultramicroscopy, 110(12): 1435-1442.